## Slide 1
Chapter 5
Failures Resulting from Static Loading
Lecture Slides
© 2015 by McGraw-Hill Education. This is proprietary material solely for authorized instructor use. Not authorized for sale or distribution in any manner. This document may not be copied, scanned, duplicated, forwarded, distributed, or posted on a website, in whole or part.

## Slide 2: Chapter Outline

## Slide 3: Failure Examples
Failure of truck driveshaft spline due to corrosion fatigue
Fig. 5–1

## Slide 4: Failure Examples
Impact failure of a lawn-mower blade driver hub.
The blade impacted a surveying pipe marker.
Fig. 5–2

## Slide 5: Failure Examples
Failure of an overhead-pulley retaining bolt on a weightlifting machine.
A manufacturing error caused a gap that forced the bolt to take the entire moment load.
Fig. 5–3

## Slide 6: Failure Examples
Chain test fixture that failed in one cycle.
To alleviate complaints of excessive wear, the manufacturer decided to case-harden the material
(a) Two halves showing brittle fracture initiated by stress concentration
(b) Enlarged view showing cracks induced by stress concentration at the support-pin holes
Fig. 5–4

## Slide 7: Failure Examples
Valve-spring failure caused by spring surge in an oversped engine.
The fractures exhibit the classic 45 degree shear failure
Fig. 5–5

## Slide 8: Static Strength
Usually necessary to design using published strength values
Experimental test data is better, but generally only warranted for large quantities or when failure is very costly (in time, expense, or life)
Methods are needed to safely and efficiently use published strength values for a variety of situations

## Slide 9: Stress Concentration
Localized increase of stress near discontinuities
Kt is Theoretical (Geometric) Stress Concentration Factor

## Slide 10: Theoretical Stress Concentration Factor
Graphs available for standard configurations
See Appendix A–15 and A–16 for common examples
Many more in Peterson’s Stress-Concentration Factors
Note the trend for higher Kt at sharper discontinuity radius, and at greater disruption
Fig. A–15–1
Fig. A–15–9

## Slide 11: Stress Concentration for Static and Ductile Conditions
With static loads and ductile materials
  Highest stressed fibers yield (cold work)
  Load is shared with next fibers
  Cold working is localized
  Overall part does not see damage unless ultimate strength is exceeded
  Stress concentration effect is commonly ignored for static loads on ductile materials
Stress concentration must be included for dynamic loading (See Ch. 6)
Stress concentration must be included for brittle materials, since localized yielding may reach brittle failure rather than cold-working and sharing the load.

## Slide 12: Need for Static Failure Theories
Uniaxial stress element (e.g. tension test)
Multi-axial stress element
  One strength, multiple stresses
  How to compare stress state to single strength?

## Slide 13: Need for Static Failure Theories
Failure theories propose appropriate means of comparing multi-axial stress states to single strength
Usually based on some hypothesis of what aspect of the stress state is critical
Some failure theories have gained recognition of usefulness for various situations

## Slide 14: Maximum Normal (Principal) Stress Theory
Theory: Yielding begins when the maximum principal stress in a stress element exceeds the yield strength.
For any stress element, use Mohr’s circle to find the principal stresses.
Compare the largest principal stress to the yield strength.
Often the first theory to be proposed by engineering students.
Is it a good theory?

## Slide 15: Maximum Normal (Principal) Stress Theory
Experimental data shows the theory is unsafe in the 4th quadrant.
This theory is not safe to use for ductile materials.

## Slide 16: Maximum Shear Stress Theory (MSS)
Theory: Yielding begins when the maximum shear stress in a stress element exceeds the maximum shear stress in a tension test specimen of the same material when that specimen begins to yield.
For a tension test specimen, the maximum shear stress is s1 /2.
At yielding, when s1 = Sy, the maximum shear stress is Sy /2 .
Could restate the theory as follows:
  Theory: Yielding begins when the maximum shear stress in a stress element exceeds Sy/2.

## Slide 17: Maximum Shear Stress Theory (MSS)
For any stress element, use Mohr’s circle to find the maximum shear stress. Compare the maximum shear stress to Sy/2.
Ordering the principal stresses such that s1 ≥ s2 ≥ s3,
Incorporating a factor of safety n
Or solving for factor of safety

## Slide 18: Maximum Shear Stress Theory (MSS)
To compare to experimental data, express tmax in terms of principal stresses and plot.
To simplify, consider a plane stress state
Let sA and sB represent the two non-zero principal stresses, then order them with the zero principal stress such that s1 ≥ s2 ≥ s3
Assuming sA ≥ sB there are three cases to consider
  Case 1: sA ≥ sB ≥ 0
  Case 2: sA ≥ 0 ≥ sB
  Case 3: 0 ≥ sA ≥ sB

## Slide 19: Maximum Shear Stress Theory (MSS)
Case 1: sA ≥ sB ≥ 0
  For this case, s1 = sA and s3 = 0
  Eq. (5–1) reduces to sA ≥ Sy
Case 2: sA ≥ 0 ≥ sB
  For this case, s1 = sA and s3 = sB
  Eq. (5–1) reduces to sA − sB ≥ Sy
Case 3: 0 ≥ sA ≥ sB
  For this case, s1 = 0 and s3 = sB
  Eq. (5–1) reduces to sB ≤ −Sy

## Slide 20: Maximum Shear Stress Theory (MSS)
Plot three cases on principal stress axes
Case 1: sA ≥ sB ≥ 0
  sA ≥ Sy
Case 2: sA ≥ 0 ≥ sB
  sA − sB ≥ Sy
Case 3: 0 ≥ sA ≥ sB
  sB ≤ −Sy
Other lines are symmetric cases
Inside envelope is predicted safe zone
Fig. 5–7

## Slide 21: Maximum Shear Stress Theory (MSS)
Comparison to experimental data
Conservative in all quadrants
Commonly used for design situations

## Slide 22: Distortion Energy (DE) Failure Theory
Also known as:
  Octahedral Shear Stress
  Shear Energy
  Von Mises
  Von Mises – Hencky

## Slide 23: Distortion Energy (DE) Failure Theory
Originated from observation that ductile materials stressed hydrostatically (equal principal stresses) exhibited yield strengths greatly in excess of expected values.
Theorizes that if strain energy is divided into hydrostatic volume changing energy and angular distortion energy, the yielding is primarily affected by the distortion energy.
Fig. 5–8

## Slide 24: Distortion Energy (DE) Failure Theory
Theory: Yielding occurs when the distortion strain energy per unit volume reaches the distortion strain energy per unit volume for yield in simple tension or compression of the same material.
Fig. 5–8

## Slide 25: Deriving the Distortion Energy
Hydrostatic stress is average of principal stresses
Strain energy per unit volume,
Substituting Eq. (3–19) for principal strains into strain energy equation,

## Slide 26: Deriving the Distortion Energy
Strain energy for producing only volume change is obtained by substituting sav for s1, s2, and s3
Substituting sav from Eq. (a),
Obtain distortion energy by subtracting volume changing energy, Eq. (5–7), from total strain energy, Eq. (b)

## Slide 27: Deriving the Distortion Energy
Tension test specimen at yield has s1 = Sy and s2 = s3 =0
Applying to Eq. (5–8), distortion energy for tension test specimen is
DE theory predicts failure when distortion energy, Eq. (5–8), exceeds distortion energy of tension test specimen, Eq. (5–9)

## Slide 28: Von Mises Stress
Left hand side is defined as von Mises stress
For plane stress, simplifies to
In terms of xyz components, in three dimensions
In terms of xyz components, for plane stress

## Slide 29: Distortion Energy Theory With Von Mises Stress
Von Mises Stress can be thought of as a single, equivalent, or effective stress for the entire general state of stress in a stress element.
Distortion Energy failure theory simply compares von Mises stress to yield strength.
Introducing a design factor,
Expressing as factor of safety,

## Slide 30: Octahedral Stresses
Same results obtained by evaluating octahedral stresses.
Octahedral stresses are identical on 8 surfaces symmetric to the principal stress directions.
Octahedral stresses allow representation of any stress situation with a set of normal and shear stresses.
Principal stress element with single octahedral plane showing
All 8 octahedral planes showing

## Slide 31: Octahedral Shear Stress
Octahedral normal stresses are normal to the octahedral surfaces, and are equal to the average of the principal stresses.
Octahedral shear stresses lie on the octahedral surfaces.
Fig. 5–10

## Slide 32: Octahedral Shear Stress Failure Theory
Theory: Yielding begins when the octahedral shear stress in a stress element exceeds the octahedral shear stress in a tension test specimen at yielding.
The octahedral shear stress is
For a tension test specimen at yielding, s1 = Sy , s2 = s3 = 0. Substituting into Eq. (5–16),
The theory predicts failure when Eq. (5–16) exceeds Eq. (5–17). This condition reduces to

## Slide 33: Failure Theory in Terms of von Mises Stress
Equation is identical to Eq. (5–10) from Distortion Energy approach
Identical conclusion for:
  Distortion Energy
  Octahedral Shear Stress
  Shear Energy
  Von Mises
  Von Mises – Hencky

## Slide 34: DE Theory Compared to Experimental Data
Plot von Mises stress on principal stress axes to compare to experimental data (and to other failure theories)
DE curve is typical of data
Note that typical equates to a 50% reliability from a design perspective
Commonly used for analysis situations
MSS theory useful for design situations where higher reliability is desired
Fig. 5–15

## Slide 35: Shear Strength Predictions
For pure shear loading, Mohr’s circle shows that sA = −sB = t
Plotting this equation on principal stress axes gives load line for pure shear case
Intersection of pure shear load line with failure curve indicates shear strength has been reached
Each failure theory predicts shear strength to be some fraction of normal strength
Fig. 5–9

## Slide 36: Shear Strength Predictions
For MSS theory, intersecting pure shear load line with failure line [Eq. (5–5)] results in
Fig. 5–9

## Slide 37: Shear Strength Predictions
For DE theory, intersection pure shear load line with failure curve [Eq. (5–11)] gives
Therefore, DE theory predicts shear strength as
Fig. 5–9

## Slide 38: Example 5–1

## Slide 39: Example 5–1 (continued)

## Slide 40: Example 5–1 (continued)

## Slide 41: Example 5–1 (continued)

## Slide 42: Example 5–1 (continued)

## Slide 43: Example 5–1 (continued)

## Slide 44: Example 5–1 (continued)
Fig. 5−11

## Slide 45: Mohr Theory
Some materials have compressive strengths different from tensile strengths
Mohr theory is based on three simple tests: tension, compression, and shear
Plotting Mohr’s circle for each, bounding curve defines failure envelope
Fig. 5−12

## Slide 46: Coulomb-Mohr Theory
Curved failure curve is difficult to determine analytically
Coulomb-Mohr theory simplifies to linear failure envelope using only tension and compression tests (dashed circles)
Fig. 5−13

## Slide 47: Coulomb-Mohr Theory
From the geometry, derive the failure criteria
Fig. 5−13

## Slide 48: Coulomb-Mohr Theory
Incorporating factor of safety
For ductile material, use tensile and compressive yield strengths
For brittle material, use tensile and compressive ultimate strengths

## Slide 49: Coulomb-Mohr Theory
To plot on principal stress axes, consider three cases
Case 1: sA ≥ sB ≥ 0 For this case, s1 = sA and s3 = 0
  Eq. (5−22) reduces to
Case 2: sA ≥ 0 ≥ sB For this case, s1 = sA and s3 = sB
  Eq. (5-22) reduces to
Case 3: 0 ≥ sA ≥ sB For this case, s1 = 0 and s3 = sB
  Eq. (5−22) reduces to

## Slide 50: Coulomb-Mohr Theory
Plot three cases on principal stress axes
Similar to MSS theory, except with different strengths for compression and tension
Fig. 5−14

## Slide 51: Coulomb-Mohr Theory
Intersect the pure shear load line with the failure line to determine the shear strength
Since failure line is a function of tensile and compressive strengths, shear strength is also a function of these terms.

## Slide 52: Example 5–2

## Slide 53: Example 5–2 (continued)

## Slide 54: Example 5−3
Fig. 5−16

## Slide 55: Example 5−3 (continued)

## Slide 56: Example 5−3 (continued)

## Slide 57: Example 5−4
Fig. 5−17

## Slide 58: Example 5−4 (continued)
Fig. 5−17

## Slide 59: Example 5−4 (continued)

## Slide 60: Example 5−4 (continued)
Answer

## Slide 61: Failure Theories for Brittle Materials
Experimental data indicates some differences in failure for brittle materials.
Failure criteria is generally ultimate fracture rather than yielding
Compressive strengths are usually larger than tensile strengths
Fig. 5−19

## Slide 62: Maximum Normal Stress Theory
Theory: Failure occurs when the maximum principal stress in a stress element exceeds the strength.
Predicts failure when
For plane stress,
Incorporating design factor,

## Slide 63: Maximum Normal Stress Theory
Plot on principal stress axes
Unsafe in part of fourth quadrant
Not recommended for use
Included for historical comparison
Fig. 5−18

## Slide 64: Brittle Coulomb-Mohr
Same as previously derived, using ultimate strengths for failure
Failure equations dependent on quadrant
Quadrant condition
Failure criteria
Fig. 5−14

## Slide 65: Brittle Failure Experimental Data
Coulomb-Mohr is conservative in 4th quadrant
Modified Mohr criteria adjusts to better fit the data in the 4th quadrant
Fig. 5−19

## Slide 66: Modified-Mohr
Quadrant condition
Failure criteria

## Slide 67: Example 5−5
Fig. 5−16

## Slide 68: Example 5−5 (continued)

## Slide 69: Example 5−5 (continued)

## Slide 70: Selection of Failure Criteria
First determine ductile vs. brittle
For ductile
  MSS is conservative, often used for design where higher reliability is desired
  DE is typical, often used for analysis where agreement with experimental data is desired
  If tensile and compressive strengths differ, use Ductile Coulomb-Mohr
For brittle
  Mohr theory is best, but difficult to use
  Brittle Coulomb-Mohr is very conservative in 4th quadrant
  Modified Mohr is still slightly conservative in 4th quadrant, but closer to typical

## Slide 71: Selection of Failure Criteria in Flowchart Form
Fig. 5−21

## Slide 72: Introduction to Fracture Mechanics
Linear elastic fracture mechanics (LEFM) analyzes crack growth during service
Assumes cracks can exist before service begins, e.g. flaw, inclusion, or defect
Attempts to model and predict the growth of a crack
Stress concentration approach is inadequate when notch radius becomes extremely sharp, as in a crack, since stress concentration factor approaches infinity
Ductile materials often can neglect effect of crack growth, since local plastic deformation blunts sharp cracks
Relatively brittle materials, such as glass, hard steels, strong aluminum alloys, and steel below the ductile-to-brittle transition temperature, benefit from fracture mechanics analysis

## Slide 73: Quasi-Static Fracture
Though brittle fracture seems instantaneous, it actually takes time to feed the crack energy from the stress field to the crack for propagation.
A static crack may be stable and not propagate.
Some level of loading can render a crack unstable, causing it to propagate to fracture.

## Slide 74: Quasi-Static Fracture
Foundation work for fracture mechanics established by Griffith in 1921
Considered infinite plate with an elliptical flaw
Maximum stress occurs at (±a, 0)
Fig. 5−22

## Slide 75: Quasi-Static Fracture
Crack growth occurs when energy release rate from applied loading is greater than rate of energy for crack growth
Unstable crack growth occurs when rate of change of energy release rate relative to crack length exceeds rate of change of crack growth rate of energy

## Slide 76: Crack Modes and the Stress Intensity Factor
Three distinct modes of crack propagation
  Mode I: Opening crack mode, due to tensile stress field
  Mode II: Sliding mode, due to in-plane shear
  Mode III: Tearing mode, due to out-of-plane shear
Combination of modes possible
Opening crack mode is most common, and is focus of this text
Fig. 5−23

## Slide 77: Mode I Crack Model
Stress field on dx dy element at crack tip
Fig. 5−24

## Slide 78: Stress Intensity Factor
Common practice to define stress intensity factor
Incorporating KI, stress field equations are

## Slide 79: Stress Intensity Modification Factor
Stress intensity factor KI is a function of geometry, size, and shape of the crack, and type of loading
For various load and geometric configurations, a stress intensity modification factor b can be incorporated
Tables for b are available in the literature
Figures 5−25 to 5−30 present some common configurations

## Slide 80: Stress Intensity Modification Factor
Off-center crack in plate in longitudinal tension
Solid curves are for crack tip at A
Dashed curves are for tip at B
Fig. 5−25

## Slide 81: Stress Intensity Modification Factor
Plate loaded in longitudinal tension with crack at edge
For solid curve there are no constraints to bending
Dashed curve obtained with bending constraints added
Fig. 5−26

## Slide 82: Stress Intensity Modification Factor
Beams of rectangular cross section having an edge crack
Fig. 5−27

## Slide 83: Stress Intensity Modification Factor
Plate in tension containing circular hole with two cracks
Fig. 5−28

## Slide 84: Stress Intensity Modification Factor
Cylinder loaded in axial tension having a radial crack of depth a extending completely around the circumference
Fig. 5−29

## Slide 85: Stress Intensity Modification Factor
Cylinder subjected to internal pressure p, having a radial crack in the longitudinal direction of depth a
Fig. 5−30

## Slide 86: Fracture Toughness
Crack propagation initiates when the stress intensity factor reaches a critical value, the critical stress intensity factor KIc
KIc is a material property dependent on material, crack mode, processing of material, temperature, loading rate, and state of stress at crack site
Also know as fracture toughness of material
Fracture toughness for plane strain is normally lower than for plain stress
KIc is typically defined as mode I, plane strain fracture toughness

## Slide 87: Typical Values for KIc

## Slide 88: Brittle Fracture Factor of Safety
Brittle fracture should be considered as a failure mode for
  Low-temperature operation, where ductile-to-brittle transition temperature may be reached
  Materials with high ratio of Sy/Su, indicating little ability to absorb energy in plastic region
A factor of safety for brittle fracture

## Slide 89: Example 5−6

## Slide 90: Example 5−6 (continued)
Fig. 5−25

## Slide 91: Example 5−6 (continued)
Answer

## Slide 92: Example 5−7

## Slide 93: Example 5−7 (continued)
Answer

## Slide 94: Example 5−7 (continued)
Fig. 5−26

## Slide 95: Example 5−7 (continued)